## Slide 1: Inlet Manifold
Final Presentation
Julia Morris
Andrew Gorodetsky
Heidi Rausch

## Slide 2: Inlet Manifold
What are we fabricating?

## Slide 3: Diffusers
The diffusers are part of the Sedimentation tank
Need to create a line flow, instead of many point flows
Diffusers are made of 2” PVC pipe that is stretched into a thin rectangle

## Slide 4: Inlet Manifold Goals
Finding an appropriate method for diffuser fabrication
Should be relatively simple
Must be able to recreate in Honduras

## Slide 5: Methods
An easy and cheap method is needed to fabricate the new inlet manifold.
In order to do this, PVC pipe should be heated and then molded into a rectangle that is 1 cm wide with a length of 10 cm.
It was determined that PVC pipe could be heated using boiling water, a heating blanket, or a heat gun.
Both boiling water and a heat gun methods have been tested and using boiling water was the most effective.

## Slide 6: How to Shape the PVC Pipe?
Our first method was to make a mold that was made of plaster of paris and can withstand very high temperatures as well as water.

## Slide 7: How to Shape the PVC Pipe?
The next method that we tested was to use a jack system. The jack would be inserted into the PVC pipe so that the lever could be pulled down which would stretch the PVC pipe to our desired dimensions.

## Slide 8: How to Shape the PVC Pipe?
Once the mold was decided to be more effective, a new one was made of steel with the new desired dimensions.

## Slide 10
http://www.youtube.com/watch?v=lZ9EGzRt4dM&feature=channel_video_title

## Slide 11: What Worked and What Didn’t?
The boiling water method was effective in heating the PVC pipe once we found a working a hot plate.
Using an open fire would be just as effective, if not more, in getting water to boil in Honduras.

## Slide 12: What Worked and What Didn’t?

## Slide 13: What Worked and What Didn’t?
As shown by the results, using the metal mold created a more uniform PVC pipe.
The jack system, while also pretty effective, also didn’t get the PVC pipe all the way to a 1 cm width.

## Slide 14: Inlet Manifold Future Work
Figure out a way to make sure diffuser pipes are lined up when installed.
Find dimensions on pipes used in Honduras so that final outside length is 10 cm.

## Slide 15
Questions?