## Slide 1: Silicon oxide etching
Wafer: 100 mm SSP silicon wafer
Film: 540 nm wet thermal oxide
Resist: 600 nm UV-210
ARC: 62 nm AR3, etched for 1:50 with ARC-etch recipe (note: 0.65 ARC etch selectivity vs. UV210)
Chamber: cleaned with oxygen plasma for 10 minutes, seasoned with process chemistry for 3 minutes before etch. Flat to back (+y in plots).
Etched for 5 minutes. 12 locations measured on 50 micron lines with P7 profilometer before etch, after etch, and after stripping resist to give rate and selectivity
Data taken January, 2018

## Slide 2: Oxford 81 – CHF3/Ar oxide process
Selectivity vs. PR: > 10

## Slide 3: Oxford 81 – CHF3/O2 nitride process on oxide
Selectivity vs. PR: 0.90

## Slide 4: Oxford 81 – CHF3/O2 oxide process
Selectivity vs. PR: 1.55

## Slide 5: Oxford 81 – CF4 process
Selectivity vs. PR: 0.50

## Slide 6: Oxford 82 – CHF3/Ar oxide process
Selectivity vs. PR: 9.2

## Slide 7: Oxford 82 – CHF3/O2 nitride process on oxide
Selectivity vs. PR: 0.90

## Slide 8: Oxford 82 – CHF3/O2 oxide process
Selectivity vs. PR: 1.40

## Slide 9: Oxford 82 – CF4 process
Selectivity vs. PR: 0.45

## Slide 10: Silicon oxide etching
Wafer: 100 mm SSP silicon wafer
Film: 540 nm wet thermal oxide
Resist: 600 nm UV-210
ARC: 62 nm AR3, etched for 1:50 with ARC-etch recipe (note: 0.65 ARC etch selectivity vs. UV210)
Chamber: cleaned with oxygen plasma for 10 minutes, seasoned with process chemistry for 3 minutes before etch. Flat to back (+y in plots).
Etched for 2 minutes. 12 locations measured on 50 micron lines with P7 profilometer before etch, after etch, and after stripping resist to give rate and selectivity
Data taken January, 2018

## Slide 11: Oxford 100 – CHF3/O2 process
Selectivity vs. PR: 1.82

## Slide 12: Oxford 100 – CH2F2 high He process
Selectivity vs. PR: 2.76

## Slide 13: Oxford 100 – CHF3/O2 process
Selectivity vs. PR: 3.71